| METAL | Description of the reaction when exposed to dry air | Description of the reaction when heated in air | PRODUCTS formed when heated |
| --- | --- | --- | --- |
| Potassium | Reacts very readily forming potassium oxide | Burns vigorously with a lilac flame | Forms a white powdery solid, potassium Oxide. 4K (s)+ O2 (g) (2K2O (s) |
| Sodium | Reacts very readily forming sodium oxide | Burns vigorously with an orange flame | Forms a white powdery solid, sodium Oxide. 4Na (s) + O2 (g) ( 2Na2O (s) |
| Calcium | Reacts readily to form coating of calcium oxide | Burns very easily with a brick red flame | Forms a white powdery solid, calcium oxide. 2Ca (s)+ O2 (g) ( 2CaO (s) |
| Magnesium | Reacts slowly to form a coating of magnesium oxide | Burns very easily with a bright white flame | Forms a white powdery solid,magnesium oxide. 2Mg (s) + O2 (g) ( 2MgO (s) |
| Aluminium | Reacts slowly to form a thin coating of aluminium oxide | Burns when heated strongly, especially if powdered | Forms a white powdery solid, aluminium Oxide. 4Al (s) +3O2 (g) ( 2Al2O3 (s) |
| Zinc | Reacts very slowly to form a thing coating of zinc oxide | Burns when heated strongly, especially if powdered | Forms a white powdery solid, zinc oxide, Which is yellow when hot. 2Zn (s) + ) + O2 (g) ( 2ZnO (s) |
| Iron | Does not react with dry air | Burns when heated strongly, especially if powdered | Forms a black powdery solid, iron (ii, iii) Oxide. 3Fe (s) ) +2O2 (g) ( Fe2O3 (s) |
| Copper | Does not react with dry air | Does not burn when heated, but does form an oxide coating if heated very strongly | Forms a black solid, copper (ii) oxide. 2Cu (s) + O2 (g) (2CuO (s) |
| Silver | Does not react with dry air | Does not burn when heated, but does form an oxide coating if heated very strongly | --------- |